ECE 440: Lecture 12

Quasi-Fermi Levels; Photoconductivity

Ex: Assume p-doped GaAs sample with 1015 cm-3 acceptors. Flash light (on/off) to initially produce Δn = Δp = 1014 EHPs/cm3 at t=0. Recombination lifetime τ = 10 ns. How do p(t) and n(t) evolve with time?

Generation processes:

Recombination processes:

Thermal equilibrium: generation = recombination

Steady-state: all time derivatives = 0

Ex: A sample of Si doped with NA = 1016 cm-3 boron, with recombination lifetime τ = 1 (s.  It is exposed continuously to light, such that electron-hole pairs are generated throughout the sample at the rate of 1020 per cm3 per second, i.e. the generation rate GL = 1020/cm3/s.

- What are equilibrium n0 and p0 (before light is on)?

- How many extra δn and δp are there with light on?

- What are the total carrier concentrations with light on?

- What is the np product?

So far: Fermi level (EF) has been an equilibrium quantity which gave us n and p, like:

Q: What does the Fermi level look like when we have excess carriers (from light), and hence non-equilibrium?

A:

But we like similar (easy) equations, so we define quasi-Fermi levels Fn and Fp:

Ex: Calculate and draw quasi-Fermi levels from the previous example.

Last but not least. We have all these excess carriers with the lights ON. Does the conductivity (resistivity) change?

Remember: σ = q(μnn0 + μpp0)

Often before, with lights off, we could neglect the contribution of the minority carriers if the sample was reasonably doped n- or p-type.

But with lights ON, we have extra carriers δn and δp such that n and p are affected:

Photoconductivity = change in conductivity due to excess carriers (EHPs) from lights being turned on: