ECE 440: Lecture 19

Current Flow in P-N Diode

Last time, we talked about unbiased p-n junction.

Today: biased (Vext ≠ 0) p-n junction & current flow.

Draw equilibrium (V=0) band diagram:

Recall built-in voltage and depletion region width:

Qualitative band diagrams with applied voltage:

Current flow in equilibrium (V=0):

Qualitative current flow:

Qualitatively expect I-V curve to be:

In forward bias, inside space charge region (SCR):

Where V is the applied bias and _______________________.

Let’s look at the injected minority carriers:

On the n-side, injected holes.

Just at the edge of the depletion region on the n-side:

Excess injected holes diffuse into the n-side:

(the same is true of excess injected electrons on p-side).

Injected hole diffusion current:

Where equilibrium hole concentration pn0 =

(and similar for injected electron diffusion on p-side, just replace subscripts p with n).

Hole diffusion current proportional to excess hole concentration at any distance x into the n-type region.

Due to hole current continuity, we can evaluate at x = xn0 = 0

We can also write diffusion current for electrons in p-side:

Now total current

J =