ECE 440: Lecture 35

Short-Channel MOSFET and Non-Ideal Behavior

Recap the “long channel” MOSFET on one page:

ID ≈ W × charge sheet × velocity (cm × C/cm2 × cm/s = C/s = A)

For VD ≥ VGS – VT the channel gets “disconnected” from VD, and only a function of VD,sat = VGS – VT.

The “short channel” MOSFET.

Modern devices L ≈ 35 nm, so at VD ≈ 1 V ( E ≈ 3×105 V/cm

Carrier velocity is almost always saturated! vsat ≈ 107 cm/s

So if the drain current ID ≈ W × charge sheet × velocity

Then approximately:

Last result is a bit counterintuitive, but pretty important!

- ID,sat proportional to (VGS – VT) rather than (VGS – VT)2

- ID,sat is practically independent of L!

- So to get more current, scale ____________ instead of L

Luckily, we do get one break as devices get smaller = velocity overshoot:

- For very short L (~ 10–50 nm) some electrons travel across the channel without _____________________

- Those “ballistic” electrons can achieve v > vsat

- This effectively raises the collective vsat > 107 cm/s   (~30% increase for 100 nm NFET, more if shorter)

What about the weak dependence of ID,sat on VDS?

This is due to “channel length modulation” ( L’ = L – ΔL

Where ΔL α (VDS – VDS,sat)

What if I keep increasing VD and/or decreasing L?

A note on the threshold voltage VT. So far, we’ve defined it for the MOS capacitor, with respect to the substrate voltage.

The (gate) voltage needed to reach charge inversion:

VT = VFB + surface potential + Qsub/Cox

What if I apply a back (substrate) voltage vs. the source?

If VSB < 0 then source/back p-n junction is _______________

If VSB > 0 then source/back p-n junction is _______________

And the depletion region around the channel _____________

Hence Qsub/Cox above ___________

And rewrite the threshold voltage taking this into account:

Note that VT is a function of VSB!

When the source-body p-n junction is reverse biased, |VT| is _________________.

This gives us a way to electrostatically control VT, and therefore the onset of the transistor “on” or “off” state.

A note on sub-threshold behavior. So far, we’ve assumed no channel current (ID=0) if VGS < VT. This is incorrect.

If ϕS > ϕF, there is some (weak) inversion charge at the surface, which gives rise to sub-threshold current flowing between the source and drain:

Where m is ___________________.

Note exponential dependence on voltages, suggesting ID below threshold is in fact limited by __________________.

Define sub-threshold slope, S:

Typical value: 70–100 mV/decade. Want it small! (why?)

Transistor constant-field scaling (Dennard’s Law)

VT design trade-off:

- High ON current ID α (VDS – VT)n requires ________ VT

- Low OFF current requires _________ VT

Since VT cannot be scaled down aggressively, the power-supply voltage (VDD = max VDS) has not been scaled down in proportion to the MOSFET dimensions:

CMOS scaling and the power crisis:

# Text boxes

Note, in “saturation”:

- ID does not increase as VGS2

- ID remains a (weak) increasing function of VDS (remember B.I.G…. mo’ voltage mo’ current).