ECE 440: Lectures 28-29

All Modes of BJT Operation

So far we’ve studied the BJT only in the “normal active” mode (VEB > 0 forward biased, VCB < 0 reverse biased). Here, well-designed device → high gain (β = 50-300); most useful.

What about operation under other bias conditions?

“Inverted” mode: CB forward-biased, EB reverse-biased.

“Cut-off” mode: both junctions reverse-biased. Negligible currents (~ 1 pA), nearly an open circuit → useful.

“Saturation” mode: Both EB and CB junctions are forward-biased, Base is flooded with minority carriers, i.e. _________ for a P+NP transistor.

- No isolation, slow recovery, in practice → avoid.

- But, useful to study because it is a superposition of “forward” and “inverted” modes of operation and leads to the more general Ebers-Moll model for the BJT.

We can still write down the minority carrier concentration in the Base, at the E and C side:

ΔpE =

ΔpC =

Where pn = __________.

So I can write the hole diffusion current in the Base:

And the Base current due to recombination:

Key observation: minority carrier diffusion equation is linear, so all BJT operation modes can be written as a superposition of the “normal active” and “inverted” modes.

Note, IC and IE can have either sign depending on voltages.

This leads to the Ebers-Moll model, the bipolar transistor as two coupled p-n diodes.

Where keep in mind that, e.g., ΔpE/pn = (eqVEB/kT - 1), etc, so:

The normal and inverted current transfer ratios αN and αI, respectively. Defined, e.g., ICp = αNIE.

IES = Emitter saturation current with C-B junction shorted.

ICS = Collector saturation current with E-B junction shorted.

Another way to think about it:

IC = C-B diode current + fraction of E-B diode current that makes it to the C-B junction.

IE = E-B diode current + fraction of C-B diode current that makes it to the E-B junction.

What approximation is always OK to make when, e.g., VEB ≫ kT/q (= ______V at room temperature)?

Ex: Common-Emitter configuration:

Draw circuit:

Draw current-voltage diagram:

- At low VEC both CB and EB diodes are ______________. Consequently the transistor is in _______________.

- At higher VEC, CB diode goes into deeper and deeper reverse bias, and EB stays forward-biased with roughly constant VEB ≈ ________.

As the CB diode is pushed into deeper reverse bias, the CB depletion region ____________________.

This effectively modulates (decreases) the _______________.

Which also modulates (increases) the ______________.

Ideally, we do not want the gain to change due to Base width modulation. During design, we have three options:

- Increase the Base width, WB

- Increase the Base doping, NB

- Decrease the Collector doping, NC

Which one is the most acceptable in practice?

What if we really push VEC until the transistor breaks?

- Punch-through (WB → 0)

- Avalanche breakdown

# Text boxes

Experimental Data

VEC

VEC [V]