ECE 440: Lecture 21

P-N Diode Breakdown

Zener breakdown:

- Dominant for heavily doped (>1018 cm-3) p+n+ diodes

- Breakdown at a few volts (typically < 5 V)

- Electron tunneling from filled valence states on p-side into (mostly) empty conduction band states on n-side

Avalanche breakdown:

- More lightly doped junctions (< 1017 cm-3)

- Wider depletion region, electrons accelerated across it gain enough energy to create additional EHPs

- Impact ionization and carrier multiplication

Empirical observations of VBR with doping and material:

- VBR decreases with increasing N (=NA or ND)

- VBR decreases with decreasing EG

Breakdown dependence on temperature:

- For tunneling (Zener) breakdown…

- For avalanche breakdown…

Two diode applications:

- Photodiode/solar cell

- Light-emitting diode (LED)