## Slide 1: NEMO5 Tutorial: Graphene Nanostructures
NCN Summer School 2012
Junzhe Geng, NEMO5 team

## Slide 2: Graphene and transistor
Advantages:
High intrinsic mobility (Over 15,000 cm2/V-s)
High electron velocity  Good transport
2D material  Good scalability
Frank Schwierz, Nature Nano. 5, 487 (2010)
100GHz Graphene FET
Image credit: IBM
Image from: University of Maryland
Akturk, JAP 2008
Shishir, JPCM 2009
CNT (Perebeinos, PRL 2005)

## Slide 3: Outline
Tutorial Outline:
  Tight binding surface treatment in NEMO5
  Graphene models, lattice, setup in nemo5
  Example 1: Graphene bandstructure, band model comparison
  Example 2: Armchair graphene nanoribbon
  Exercise: Zig-zag graphene nanoribbon
  Example 3: Graphene nanomesh with a circular hole
  Exercise: Graphene nanomesh with a rectangular hole

## Slide 4
Surface Treatment
In NEMO5

## Slide 5: Surface Passivation in NEMO5: example Si UTB
Example: Si_UTB_10uc_no_pass.in
10 unit cell
Inputdeck: Bandstructure calculation of a Si UTB with default settings, no passivation used
passivate = false

## Slide 6: Surface Passivation in NEMO5
Example: Si_UTB_10uc_no_pass.in
10 unit cell
UTB Bandstructure:
A few states span over the band gap
Identify the nature of band gap states:
Get the wave functions
Calculate the wave functions at the Γ point

## Slide 7: Surface Passivation in NEMO5
Example: Si_UTB_10uc_no_pass.in
10 unit cell
10 unit cell
Surface state
Volume state
States in the bandgap are surface states They are produced by dangling bonds

## Slide 8: Surface Passivation in NEMO5
Example: Si_UTB_10uc_pass.in
10 unit cell
“passivate = true”
Adds H-atoms at the surface

## Slide 9: Surface Passivation in NEMO5
Example: Si_UTB_10uc_pass.in
10 unit cell
Surface states are shifted out of band gap region to very high energies (~1 keV)

## Slide 10
Graphene
http://en.wikipedia.org/wiki/Graphene

## Slide 11: Tight-binding Model
pz orbital is well separated in energy from the sp2 orbitals
More importantly, only the pz electron is close to the Fermi level
Therefore, the common tight-binding method for graphite/graphene considers only the pz orbital (P.R. Wallace, PRB 1947)
2s
2pz
2py
2px
2pz
sp2
Y. Zhang and R.Tsu, Nanoscale Research Letters Vol. 5 Issue 5

## Slide 12: Passivation in PD and Pz tight binding model
NEMO5: two models for Graphene bandstructure
Standard model of tight binding literature “Pz”
Includes just one pZ orbital per atom
Does not allow for hydrogen passivation
Because pz orbital of C has zero coupling to s orbital in H
pZ
pZ
dyz
dzx
Recently developed model “PD” (J. Appl. Phys. 109, 104304 (2011)
Includes {pz dyz dzx} orbital set on each C atom and H atom
Hydrogen atoms included explicitly (realistic treatment)
“passivate_H” not required in job_list
BUT
Make H atoms “active”, i.e. include them explicitly:
Domain
{
activate_hydrogen_atoms = true (default = false)
Always have passivate = true in the domain section (default)

## Slide 13: Graphene: Primitive Basis
A1
A2
Γ
M
K
a1
a2
a0= 0.142nm
Lattice basis:
Reciprocal lattice basis:
Symmetry points:
Given in NEMO5
User defined points

## Slide 14: Defining the Structure
‘primitive’ or ‘Cartesian’
Define the material
With a large enough region, device is limited by dimension only
Dimension in number of unit cells
Have “true” only for PD model

## Slide 15: Defining Solver
Expressed in units of A1 and A2
‘Pz’ or ‘PD’
A1
A2
Γ
M
K
Symmetry points:
Γ  K  M  Γ

## Slide 16: Graphene Bandstructure: PZ vs. P/D
DFT results are much better reproduced with the PD model
NEMO5
pz
p/d
J. Appl. Phys. 109, 104304 (2011)
Boykin et al.

## Slide 17
Graphene Nanoribbons
Z.Chen, et al. Physica 40, 228-232 (2007)

## Slide 18: Graphene: Cartesian Basis
A1
Γ
a1
a2
A2
Lattice basis:
Reciprocal lattice basis:
a0= 0.142nm

## Slide 19: Structure
cartesian
a1
a2
A1
A2

## Slide 20: Example 1 : 10-AGNR
x
y
“Armchair”
10 atomic layers wide
Periodic
A big domain

## Slide 21: 10-AGNR Bandstructure
bandgap
Armchair edges allow opening up a bandgap

## Slide 22
Exercise: Define a “10-ZGNR” in NEMO5 and calculate its bandstructure along x direction ([100])
1
2
3
4
9
10
“zigzag”
y
x
a1
a2
a0= 0.142nm

## Slide 23: Exercise1 : 10-ZGNR
y
x
1
2
3
4
9
10
“zigzag”

## Slide 24: Bandstructure: 10-ZGNR
Zigzag edges give metallic behavior

## Slide 25
Graphene Nanomeshes
J. Bai et al. Nature Materials 5, 190-194 (2010)
http://today.ucla.edu/

## Slide 26: Example 2: Graphene Nanomesh
12 unit cell
12 unit cell
7 unit cell
Region 1 defines the graphene supercell
Region 2 defines a hole
Higher priority in the hole region
Only include region 1 in the domain

## Slide 27: Bandstructure: GNM
Need to visualize the wavefunction at the Γ point
Flat bands in the middle of the bandgap
Eg = 0.75 eV
12 unit cell
12 unit cell
7 unit cell

## Slide 28: Wavefunction Visualization
A new directory
That stores all wavefunction files

## Slide 29: GNM: Edge state
High
Low
Localized state
Propagating state
zigzag
d = 7 uc
Wavefunctions on the flat band are localized at the zigzag edges

## Slide 30: Exercise 2: Graphene Nanomesh
Exercise:
Define a graphene nanomesh of 8nm x 8nm with rectangular hole 7nm x 1nm.
Plot bandstructure along x and y.
Obtain and visulize wavefunctions at Γ point
8nm
7nm
1nm
8nm
a1
a2
a0= 0.142nm
y
x

## Slide 31: Exercise 2: Graphene Nanomesh
8nm
7nm
1nm
8nm
Structure:

## Slide 32: Bandstructure and Wavefunctions
Edge state at the zigzag edges
[100]
[010]
High
Low

## Slide 33
Thank you !

## Slide 34: Example 2: Graphene Nanomesh
Material is only defined for region 1
12 unit cell
12 unit cell
5 unit cell
Hole defined here:

## Slide 35: Bandstructure: GNM
How can we visualize electron wavefunctions at Gamma point?

## Slide 36: Wavefunction Visualization
A new directory
That stores all wavefunction files

## Slide 37: Wavefunction Visualization
Wave functions are
centered at edges (zigzag edges)
spread out over the total sheet