## Slide 1: Using NEMO5 to quantitatively predict topological insulator behaviour
Parijat Sengupta, Tillmann Kubis, Michael Povolotskyi, Jean Michel Sellier, Jim Fonseca,
Gerhard Klimeck
Network for Computational Nanotechnology (NCN) Electrical and Computer Engineering Purdue University, West Lafayette IN, USA
psengupta@purdue.edu
Summer School 2012

## Slide 2: Some commonly known facts
*Wikipedia
*

## Slide 3: A dispersion cartoon
Conduction band
Valence band
Eg
An insulator such as SiO2, Si3 N4 with
large band-gap
Conduction and Valence bands describe electrons and holes
The band gap is zero in a metal
Some materials possess the dual properties of metals and insulators
We will use NEMO5 to investigate some of these unique materials

## Slide 4: What are these materials?
Primary examples are Bi2Te3 , Bi2Se3 , BixSb1-x etc…
They are known as topological insulators
These materials contain bound surface states
sp3d5s* tight binding calculation
Dispersion obtained through ARPES*
Dirac Cone
ε
κ
*Rev of Mod. Phys, Vol 82, Oct-Dec 2010

## Slide 5: Setting up the simulation task
sp3d5s* tight binding calculation
Dirac Cone
We will use a sp3d5s* tight binding model
Bi2Te3 is our topological insulator material
A 9 nm (appx) long quantum well will be the target device
This will produce a band structure as shown on left
Key feature of this dispersion is a graphene-like linear character (Dirac cone)
Linearity is not due to same reason as in graphene!

## Slide 6: Details of the simulation structure
Z-axis : Confined
X & Y axes : Periodic
9 nm wide c-axis oriented Bi2Te3 thin film
Different surface termination: Surface 1 (2) is Bi (Te2) terminated
Te terminated surface
Bi terminated surface
Bi
Te1
Te2
periodic
periodic

## Slide 7: The NEMO5 input deck skeleton
There are 3 blocks in the input deck:
Structure
{
}
Solvers
{
}
Global
{
}
Defines material and simulation domains
Sets up simulations that has to be solved, e.g. equations,
boundary conditions, iterative processes, output,
numerical options, etc.
Defines global variables such as temperature, which database file to use, diagnostic output, etc.

## Slide 8: The NEMO5 input deck: The first block “Structure”
Structure
{
}
Domain
{
name = device
…
}
Domain
{
name = contact1
…
}
Geometry
{
}
Material
{
name = XYZ
…
}
Material
{
name = ABC
…
}
Materials
Domains for simulations
Description of the geometry

## Slide 9: Setting the input deck…
Every input deck begins with the Structure group
Each region is identified by a name known as the tag
The underlying crystal structure of the material needs to be provided
Each simulation can have multiple regions, NEMO5 needs the exact number of those for correct execution
The surface atoms can be controlled by asking NEMO5 to place a specific atom when constructing the first unit cell

## Slide 10: Defining parameters and the domain
Any parameter defined in the input deck takes precedence over the corresponding database entry
Dimension creates a canvas of unit cells
Periodicity set as false refers to a confined axis  k is not a good quantum number
Passivate options allows inclusion of Hydrogen atoms

## Slide 11: Crystal orientation in NEMO5
Crystal directions set up the coordinate system within the crystal using the basis vectors
The basis vectors are aligned to the Cartesian axes through the space orientation option
In this example: crystal_direction1 = (0,0,1) is aligned along space_orientation_dir1 = (0,0,1) or the z-axis.
You need to specify only 2 directions. N5 computes the third using the crystal structure info.
space_orientation_dir1 is the z-axis and is confined: the first entry of periodic option

## Slide 12: “crystal_direction” & “space_orientation”: A closer look
What NEMO5 internally produces ?
It produces three basis vectors
These basis vectors can be obtained by examining the first three lines of the device_coupling.dat file
To obtain this file, include output = (xyz, coupling) in the Domain section. You will see an example of it in your first exercise
Three vectors in the device_coupling.dat file
a = [0 0 3.0487]
b = [0.4383 0 0]
c = [-0.2191 0.3796 0]
How do you check that these vectors make sense?
All length units are in nm

## Slide 13: Reconciling results to known crystal geometry
Three vectors in the device_coupling.dat file
a = [0 0 3.0487]
b = [0.4383 0 0]
c = [-0.2191 0.3796 0]
Our test case here is Bi2Te3 which has a hexagonal base
Each edge of hexagon is 0.4383 nm
Two hexagons are displaced along z-axis by 3.0487 nm
b
c
Norm of vectors b and c is equal to 0.4383 nm
Norm of vector a is equal to 3.0487 nm
Angle between b and c is 1200 as expected
Check:
Hexagonal base of Bi2Te3 quintuple layer
The vectors b and c have an 120 degree angle between them

## Slide 14: The actual geometry in numbers
Shape options allows you to input a geometric shape for your device
Setting the priority gives you control over structure creation when dealing with composite geometric shapes.
Higher priority gets constructed first
Actual device size is specified through min & max

## Slide 15: The NEMO5 input deck skeleton
There are 3 blocks in the input deck:
Structure
{
}
Solvers
{
}
Global
{
}
Defines material and simulation domains
Sets up simulations that has to be solved, e.g. equations,
boundary conditions, iterative processes, output,
numerical options, etc.
Defines global variables such as temperature, which database file to use, diagnostic output, etc.

## Slide 16: Executing the input deck: The solvers!
Each solver has a name
The first solver (usually) is the geometry constructor
The atomic coordinate positions are dumped out in a structure file
The structure file can have several formats such as vtk, silo, xyz, pdb…

## Slide 17: Electronic structure calculation options - I
Electronic structure calculation must set the type to Schroedinger
job_list shows what actions N5 must perform
Setting orbital_resolved to true shows the contribution of each orbital to overall band structure

## Slide 18: Electronic structure calculation options - II
tb_basis option lets you choose the band structure calculation model.
tb_basis can also be set to effective mass (em)
k_space_basis can also be set to Cartesian
Number of nodes  Number of k-points in the chosen k interval

## Slide 19: The NEMO5 input deck skeleton
There are 3 blocks in the input deck:
Structure
{
}
Solvers
{
}
Global
{
}
Defines material and simulation domains
Sets up simulations that has to be solved, e.g. equations,
boundary conditions, iterative processes, output,
numerical options, etc.
Defines global variables such as temperature, which database file to use, diagnostic output, etc.

## Slide 20: Putting it all together…
The global section has the command solve: All job names are included under solve
database is custom built for N5 and contains all material parameters
messaging level indicates code progress output on screen. Level 5 is verbose

## Slide 21: Exercise -I
Log in to your workspace account and create a folder TI in your home directory. Navigate to the TI folder
mkdir TI
cd TI
Pull the necessary files in your TI folder by typing the following :
cp ../public_examples/NCN_summer_school_2012/
Topological_Insulators_psengupta/ex*.in .
cp ../public_examples/NCN_summer_school_2012/
Topological_Insulators_psengupta/spin_analysis_ex*.m .
ex1.in is the input file to calculate the dispersion relationship for a 9.0 (appx) long Bi2Te3 quantum well
Submit a job by typing the command :
submit -v ncn-hub@coates -i ../all.mat -n 16 -N 8 nemo-r8028 ./ex1.in

## Slide 22: What do you expect to see as a solution?
Band structure for a 9.0 nm long Bi2Te3 quantum well
NEMO5 will produce four files (SS12_TI_ex1_*.dat)
Start MATLAB on your workspace
Your folder has a MATLAB file called spin_analysis_ex1.m
Execute the MATLAB script by typing spin_analysis_ex1 at the command prompt
You will have the figure on your left!
To run Matlab:
$ use matlab-7.12
$ matlab

## Slide 23: Exercise –I contd…
Supplementary exercise :
Change line 20 of the spin_analysis_ex1.m file from the preset
n = [1 0 0] to n = [0 0 1] and n = [0 1 0]
Run Matlab
The three different spin-polarized plots that you obtain highlight a fundamental theory of TIs
Pre-computed results are stored in folder /public_examples/NCN_summer_school_2012/Topological_Insulators_psengupta

## Slide 24: Inter-linking solvers in NEMO5
Several solvers defined in the Solver block can be inter-linked:
Solver1
{
}
Solver2
{
}
Solver3
{
}
We will see a specific example of this coupling of solvers in the next part of the tutorial

## Slide 25: NEMO5 is a toolbox….
Update ɸ
Solvers can also speak to one another
e.g. A self-consistent charge calculation
Start
Density solver (e.g. Schrödinger)
Potential solver (e.g. Poisson (ɸ))
Conv ?
End
No
Yes
solve = (struct, schrödinger, poisson)

## Slide 26: Setting up the Poisson…
A name is assigned to the Poisson solver (similar to previous slides)
A non-linear Poisson will be solved
A continuum domain is constructed
Linear solver settings
Electrostatic output option

## Slide 27: Linking Poisson to Schroedinger…
Specific model applicable to topological insulators
Convergence criterion
The simple linking step done through inserting name of desired solver
job_list tells NEMO5 to compute specific physical quantities
For a self-consistent calculation electron density is computed

## Slide 28: A few options in the density solver
First two blocks of input statements are identical to normal eigen value calculations done earlier
threshold_energy lets you choose eigen states beginning with energy as set in the option
chem_pot is the Fermi level to start calculations
Schrodinger receives the potential from the my_poisson potential solver
More advanced calculations can use boundary condition options
Inter-linking solvers : my_poisson and BiTe_density

## Slide 29: Implementing boundary conditions
Boundary conditions can be of two forms in NEMO5.
Dirchlet (potential (ɸ) = constant)
Neumann (∂ɸ = constant)
The input deck statements shown on left can be included multiple times at all possible external boundaries
The right boundary region number must be specified
E_field allows to apply an electric field of certain magnitude to device structure. It is in units of V/cm

## Slide 30: Updating Schrödinger for eigen states calculation
Exactly same format as in Exercise 1
Potential solver is added which supplies potential to the tight - binding Hamiltonian

## Slide 31: Exercise -II
ex2.in is the input file to calculate charge self-consistent dispersion relationship for a 9.0 (appx) long Bi2Te3 quantum well
This task will produce a dispersion relationship, potential landscape, and the charge profile in the device
Submit the job by typing the command :
submit -v ncn-hub@coates -i ../all.mat -n 16 -N 8 nemo-r8028 ./ex2.in

## Slide 32: What do you expect to see as a solution?
Self-consistent band structure for a 9.0 nm long Bi2Te3 quantum well
NEMO5 will produce four .dat files (SS12_TI_ex2_*.dat) and a .xy file (poisson_ex2.xy)
Start MATLAB on your workspace
Your folder has a MATLAB file called spin_analysis_ex2.m
Execute the MATLAB script by typing spin_analysis_ex2 at the command prompt
You will have the figure on your left!

## Slide 33: Electrostatic calculations
Use the poisson_ex2.xy file (three column file) in your folder to plot the charge and potential profile
Start MATLAB on your workspace
Type the following for the charge & potential plot :
cp = load(‘poisson_ex2.xy’);
% potential plot
figure(1)
plot(cp(:,1), cp(:,2))
% charge plot
figure(2)
plot(cp(:,1), cp(:,3))
You can also use any plotting software :
Please remember : Column 1 is device coordinate followed by potential and charge data on columns 2 and 3

## Slide 34
How do the results from Exercise I and II look like?
Self-consistent electronic structure
Schrödinger 20 band tight binding
Poisson calculation has large impact:
Energy separation between Dirac cones gets enhanced
Fermi velocity of Dirac states changes (mobility)
Dirac points move below the Fermi level, into the bulk DOS

## Slide 35
Self-consistent electrostatic calculations
Bi terminated surf.
Te terminated surf.
Smooth perturbative potential
Oscillations in the potential between anion/cation covered by bulk parameters
Change of charge polarity at two surfaces due to different atomic termination
Common in TB:
Charge oscillations between atom types
Intrinsic dipole due to distinct surfaces

## Slide 36
Conclusion
Band structure calculations
  Can handle the newest materials like topological insulators
Thank you.
Charge self-consistent band structure calculation
  For accurate device prediction
Use of solvers to accomplish modular tasks
  As many solvers as needed can be added
  Solvers can be inter-linked
    Simple process accomplished by inserting appropriate solver name

## Slide 37
Crystal Structure of Bi2Te3 and tight-binding representation
quintuple layer
Te
Bi
Te
Bi
Te
Bi2Te3
Devices represented atomically in their native rhombohedral crystal structure
Electronic structure calculations with atomistic tight binding sp3d5s* 20 band model
Inequivalent Te atom
5 atom unit cell
Quintuple layer ordered as Te(1) - Bi(1) -Te(2) - Bi(1) - Te(1)
Inequivalent Te atom serves as centre of inversion