ECE 440: Lecture 2

Fall 2008, Prof. Eric Pop

Online reference:

http://ece-www.colorado.edu/~bart/book/

Crystal Lattices:

- Periodic arrangement of atoms

- Repeated unit cells (solid-state)

- Stuffing atoms into unit cells

- Diamond (Si) and zinc blende (GaAs) crystal structures

- Crystal planes

- Calculating densities

Appendix III in your book:

The periodic lattice:

Stuffing atoms into unit cells:

- How many atoms per unit cell?

- Avogadro’s number: NA = # atoms / mole

- Atomic mass: A = grams / mole

- Atom counting in unit cell: atoms / cm3

- How do you calculate density?

The Silicon lattice:

- Si atom: 14 electrons occupying the lowest 3 energy levels:

  - 1s, 2s, 2p orbitals filled by 10 electrons

  - 3s, 3p orbitals filled by 4 electrons

- Each Si atom has four neighbors

- “Diamond lattice”

- How many atoms per unit cell?

Zinc blende lattice (GaAs, AlAs, InP):

- Two intercalated fcc lattices

Crystallographic Notation

Crystallographic planes and Si wafers

Si wafers usually cut along {100} plane with a notch or flat side to orient the wafer during fabrication

Where do (pure) Si wafers come from?

- Read sections 1.3-1.4

- Take ECE 444

- Short answer:

Source: Wikipedia