ECE 440: Lecture 5

Intrinsic Material, Doping, Carrier Concentrations

Intrinsic semiconductor = pure, without external additives

No charge carriers at T=0K

What about at T=300K?

How much energy to break a bond?

What is created when a bond is broken by thermal agitation?

How many?

In thermal equilibrium, generation = recombination

Simple probability:

Recombination driven by…

Generation intrinsically driven only by…

Hence, the np product at thermal equilibrium:

So what is np numerically? (a peek ahead)

At room temperature (T=300K), intrinsic concentrations:

ni  ~ 	2 x 106 electrons and holes per cm3 in GaAs

1 x 1010 cm-3 in Si

2 x 1013 cm-3 in Ge

What about band gaps?

How do these numbers compare with NA?  With the number of silicon atoms per cm3 (x4 valence electrons per atom)?

Q: Does an intrinsic semiconductor, at room temperature, spontaneously emit light? Why/not?

What if temperature is increased?

Manipulating carrier concentrations.

Extrinsic material.

Doping = purposely introducing impurities into the crystal.

Donors and acceptors (of what?)

Ex: compare number of valence electrons (e.g. 5 for As) with the number of electrons of the atom it replaces (e.g. 4 for Si).

Arsenic (As) in Si: 4 electrons for bonding with neighbors.  But, how loosely bound is that 5th electron that As brought into the Si lattice?

Use approximation from N. Bohr’s model:

(be careful with choice of m* and K)

On homework: calculate Bohr radius, a.k.a. fuzzy electron orbit radius around donor atom.

The real numbers for donors and acceptors in Si:

| Donor in Si | P | As | Sb |
| --- | --- | --- | --- |
| Binding energy (eV) | 0.045 | 0.054 | 0.039 |

| Acceptor in Si | B | Al | Ga | In |
| --- | --- | --- | --- | --- |
| Binding energy (eV) | 0.045 | 0.067 | 0.072 | 0.16 |

How do these donor & acceptor binding energies look like in the band diagram model?

Recall: thermal agitation energy ~ 3/2 kBT

Extrinsic:

N-type semiconductor =

P-type semiconductor =

Ex: What are the electron & hole concentrations in a Si wafer doped with 1015 cm-3 As atoms (at room temperature)?  Is this n- or p-type Si?

How much has the resistivity of Si changed from intrinsic?

What if I increase the temperature by 60 oC?