ECE 440: Lectures 22-23

P-N Junction Capacitance; Contacts

In reverse bias (V<0) fixed charge is stored in the junction, as the depletion width widens with more negative V. Why? How does W change with voltage?

If I measure and plot 1/CJ2 vs. V, I can get ______________

Example: Given the slope (1/CJ)2 vs. voltage is -2e23 F-2V-1, the intercept is 0.84 V, and the diode area 100x100 μm2. If NA ≫ ND, find the two sides’ doping concentrations.

We’ve (nearly) exhausted the p-n junction. Now we know:

- Why and how it conducts current (forward, reverse)

- How to calculate depletion width, field, built-in voltage

- How to make an LED or photodiode

- How diodes break down

- How diodes store charge as capacitors

But, real semiconductors devices and chips always contain metals. Why? _______________________________

Metals are easier than semiconductors:

- No band gap, only Fermi level matters

- ~ 100-1000x more electrons than highly doped silicon (will there be any depletion on the metal side of a metal-silicon junction?)

Draw metal next to semiconductor, define work function:

Another scenario, if Φm < Φs

Example: calculate semiconductor work function qΦs if it is silicon doped p-type with NA = 1017 cm-3.

Two types of metal-silicon contacts become apparent:

- Schottky (rectifying, like a diode)

- Ohmic

How do you get one vs. the other?

A:

When would you want one vs. the other?

A:

Silicon work function:

Some typical metal work functions:

Schottky (rectifying) contact on n-type silicon.

Apply + voltage on metal, reduce built-in energy barrier.

What happens?

Can electrons flow from metal to silicon?

Apply – voltage on metal, enhance built-in energy barrier.

Ohmic contact on silicon.

Two ways to achieve them:

- Choose metal with appropriate work function to “match” the Fermi level of p- or n-type silicon

- Dope silicon highly, to thin out Schottky barrier, so electrons can tunnel through (almost) regardless of Φm